## Slide 1: Materials for Extreme Environments
Hypervelocity Impacts
6.3 km/s HVI to 0.17 in Thick Carbon Composite Projectile: 4 mm Al 2017-T4 Sphere
Multiscale Modeling - GraFEA
4.8 km/s HVI to UHMWPE Projectile: 10 mm Al 1050 Sphere (HVIL-0017)
Advanced Diagnostics for Fragmentation Tracking

## Slide 2: Materials for Extreme Environments Team
Dr. Thomas Lacy
Professor
telacyjr@tamu.edu
Dr. Raj Kota
BCDC Research Engineer
kkraj@tamu.edu
Dr. Justin Wilkerson
Assistant Professor
wilkerson@tamu.edu
Dr. J.N. Reddy
Distinguished Professor jnreddy@tamu.edu
Dr. Waruna Kulatilaka
Associate Professor
waruna.kulatilaka@tamu.edu
Dr. Arun Srinivasa
Holdredge/Paul Professor arun.r.srinivasa@tamu.edu
Dr. Prakash Thamburaja
Visiting Professor prakash.thamburaja@tamu.edu
Matthew Hay
BCDC Research Fellow
Jacob Rogers NSF GRFP Fellow
Paul Mead DoD Smart Scholar
Khari Harrison
James Leaverton
Gavin Lukasik
Aniket Mote
Carson Lawrence
Ho Yong Shin
Nathaniel Bass
Joey Stricklin
Cullen Miller

## Slide 3: State-of-the-Art Dynamic Materials Testing & Characterization T.E. Lacy, K.R. Kota, W. Kulatilaka, J.N. Reddy, A. Srinivasa, J. Wilkerson
TAMU HVI laboratory provides a test bed for development and tailoring of novel structures comprised of advanced materials, including metals, composites, polymers, ceramics, and geomaterials
  2SLGG*, High speed imaging (10M fps)*, laser based-diagnostics*, flash x-ray*, thermal imaging, photon Doppler velocimetry, etc.
Projectile
Velocity: 2-8 km/s (4,400-18,000 mph)
Size: 2-10 mm (0.08-0.40 in)
Shape: cylindrical, spherical, ogive, buckshot
Target Specimen
Impact angle: 0-90°
Maximum size: 0.6 m x 0.6 m (2’ x 2’)
Maximum weight: ~90 kg (200 lb)
Saboted Projectile
Future Plans: Establish suite of experimental capabilities (drop tower*, traditional Kolsky bar, miniature Kolsky bar*, flyer plate impact, and HVI testing*) that enable materials characterization over a wide range of strain rates (102-107). (*existing)
“Bear”
2SLG - Gun Dog
TAMU Laboratory for Nonequilibrium Phenomena: https://www.neplab.net/
TAMU Optical Diagnostics and Imaging Laboratory: https://laserlab.tamu.edu/

## Slide 4: TAMU HVI Testing: A Perspective
45º 2 km/s HVI to 4 mm Thick SiC Coated Carbon Composites Projectile: 4 mm diameter Nylon 6/6 Sphere
45°
XXX km/s HVI to PC followed by ballistic gel Projectile: 4 mm diameter Al 2017-T4 Sphere
2.5 km/s HVI to Water Droplets Projectile: 12.7 mm diameter PC Cylinder
Normal 6.6 km/s HVI to 6.35 mm Thick HDPE Projectile: 12.7 mm diameter Polymer Cylinder
Normal 2 km/s HVI to 3 in Thick High-Performance Concrete Projectile: 10 mm diameter S2 Steel Sphere
Normal 2.6 km/s HVI to 6.35 mm Thick UHMWPE Projectile: 10 mm diameter 1050 Al Sphere
60º 5.4 km/s HVI to 6.35 mm Thick HDPE Projectile: 10 mm diameter 1050 Al Sphere
6.9 km/s HVI to 4 mm Thick Stitched Carbon/Epoxy Projectile: 6 mm diameter Al 2017-T4 Sphere

## Slide 5: 5/25 Meeting
record more data points (ongoing)
  2 data points last week (both 4 mm @ ~ 6000 at 125 torr), very low variance by visual examination
  may have trouble convincing anyone to let me use an even slightly risky backfill for their shot
optimization of tests for test matrix (completed)
  will continue to procedurally update test matrix based on results
send all docs to jacob (done)
look up statistical methods and requirements (done)
  model should hold up to review
edit thesis word doc and begin transfer to LaTeX (done)

## Slide 6: 6/8 Meeting
lit review (ongoing)
  collected some articles to review, found some good info to cite for the statements I made in the paper
  organized Mendeley
figures for paper
  give feedback (done)
  make changes (ongoing)

## Slide 7: 6/15 Meeting
examine paper content and determine which figures are appropriate
thesis content vs journal paper
think of a better term for sabot stripper
  literature refers to it as sabot stripper/sabot stripper plate
  opportunity to rename it something cool

## Slide 8: Future/TODO
3D scan/measure 10/6/4 mm sabots to find center of mass for rotation arguments (TODO)
add in more analysis to the paper based on lit review / further investigation (TODO)

## Slide 9: Figure 1
Downrange
Uprange
Target Tank
Blast Tank
Flight Tube
Central Breech
Pump Tube
Powder Breech
13.7 m
1.2 m
Muzzle
Sabot stopping plate
2.4 m
Figure 1: The two-stage light gas gun (2SLGG), with necessary dimensions, located in the TAMU HVI Laboratory. The key components of concern in this work are the muzzle, blast tank, and sabot stopping plate (SSP).
y
z

## Slide 10: Table 1
Property | 4 mm sabot | 10 mm sabot
Mass (g) |  | 
Density (g/cc) |  | 
Volume (cc) |  | 
Material? |  | 
L/D |  | 
Aerodynamic cutout radius (mm) |  | 
Number of serrations |  | 
Table 1: A summary of key properties for both the 4 mm and 10 mm sabots.

## Slide 11: Figure 2
COMMENTS: can we replace these sabot figures with 4- and 10-mm sabot models? This will give the reader an idea of the relative size difference, as 6 mm is not even considered in the paper. Also, can you provide the figures as separate images? I will finish the figure with annotations. I omitted Figure 4 because the ideas can be combined into this figure.
(a)
(b)
(c)
(d)
(e)
(f)
10 mm
4 mm
Sabot Petal
Partially Closed Sabot
Fully Closed Sabot
45º serration
XX mm
XX mm
45º serration
10 mm projectile
10 mm projectile cavity
4 mm projectile cavity
4 mm projectile
Aerodynamic cutout
Aerodynamic cutout
12.7 mm
12.7 mm
⌀XX mm
⌀XX mm
Figure 2: Three-dimensional models of the two considered sabot configurations with dimensions and key features: (a)-(c) 4 mm sabot and (d)-(f) 10 mm sabot.

## Slide 12: Figure 3
Blast Tank
Downrange
Uprange
Sabot stopping plate (SSP)
Projectile flight path
Sabot flight path
(3)
Drift Tube
Figure 3: The main sequence of events during aerodynamic sabot separation: (1) projectile package exits the 2SLGG launch tube muzzle, (2) sabot petals aerodynamically separate from the projectile, and (3) the sabot petals impact the sabot stopping plate (SSP) as the projectile enters drift tube. Only two sabot petals are shown for visualization purposes.
(2)
(1)
y
z

## Slide 13: Figure 4
Ø31.8 mm
AoP
Figure 4: The SSP image (a) before and (b) after image processing. The photograph (a) is scaled to match the boundary, , and is converted into a binary image (b) before the boundary of each sabot impact region is traced for analysis in Python. The algorithm determines the sabot petal impact boundaries, , the centroid, of the area enclosed by , and the radius from each centroid to the Axis of Penetration,
y
x
y
x
(a)
(b)
Photograph
Binary Image
Sabot impact
Ø152.4 mm
2
4
1
2
4
1
2
3
4
1
2
3
4

## Slide 14: Figure 4
Identify the different aspects. Make sure this figure is necessary and can stand alone. What is it in this figure that makes it necessary? Why not just use Fig. 2?
Necessary to show difference in downrange end of 10/4 mm sabot. This can be combined/reconfigured to show the center of mass to demonstrate the moment of inertia

## Slide 15: Figure 4
(a)
(b)
I like figure (b), but you may want to add notes/text to indicate what the different regions mean to the reader. Also, you need to indicate that it is a sabot stripping plate. For figure (a), we need to convert from m/s to km/s, and from inches to mm. We want a white background and make the view isometric. I would also fix the gridlines so they evenly spaced. Essentially, clean up the axes.

## Slide 16: Figure 5
Change from m/s to km/s and from inches to mm.

## Slide 17: "There is nothing more fulfilling than to serve your country and your fellow citizens and to do it well.” – Pres. George H.W. Bush
Contact Information: Director Manager
Dr. Tom Lacy, MEEN Dr. Raj Kota, BCDC
TELacyJr@TAMU.edu KKRaj@TAMU.edu
(662) 948-9213 (cell) (662) 617-9196 (cell)